## Slide 1: 소재수치해석 final-term
20100091 서 현 선

## Slide 2: Ⅰ. 지정 과제 darken’s uphill diffusion

## Slide 3: ASSIGNMENT

## Slide 4: Background thermodynamics
Mathematical modeling of multicomponent diffusion coefficients
# 확산 유속은 농도 C의 기울기를 이용해 표현하지만 실제 simulation에서는 V와 C를 곱한 U-fraction을 사용!
for k  S (substitutional)
for k  S

## Slide 5: Background thermodynamics
Solution thermodynamics
# Darken의 Uphill Diffusion 실험이 이루어진 fcc Fe-Si-C 고용상에 대한 열역학 parameter (J/mol)

## Slide 6: Background thermodynamics
Solution thermodynamics

## Slide 7: Background thermodynamics
Solution thermodynamics
}

## Slide 8: Background thermodynamics
Diffusion coefficients

## Slide 9: Background thermodynamics
Finite Difference Methods
# Fick’s 2nd law :
# FDM(explicit method):
(기하평균 사용)

## Slide 10: Code structure
초기조성 wt% -> y로 변환
Update D, ysi, yc using FDM
y -> wt%로 다시 변환 후 txt 저장

## Slide 11: Key code
Si : 3.8wt%
C : 0.478wt%
Si : 0.001wt%
C : 0.441wt%
50mm
50mm
열처리 온도 : 1323K
열처리 시간 : 13days
초기조성 입력 및 wt% -> u fraction으로의 변환!
[Setting]
dx=0.001m
dt=1s

## Slide 12: Key code
…
…
Explicit method
Time limit: 13days=1123200s
Diffusion coefficients 계산

## Slide 13: Key code
다시 u fraction -> wt% 으로 변환 후 txt file 저장!

## Slide 14: results
Carbon diffusion (13days)

## Slide 15: results
시간에 따른 Carbon의 확산

## Slide 16: results
Si diffusion (13days)
Diffusion이 거의 일어나지 않음!

## Slide 17: conclusion
# FDM을 이용한 simulation을 통해 fcc Fe-Si-C 3원계 고용상에서의 carbon의 Darken’s uphill diffusion을 확인할 수 있었다!
# 확산의 driving force가 concentration gradient가 아닌 chemical potential gradient 임을 알 수 있다!(Si 농도가 더 높은 왼쪽 시편에서의 C의 chemical potential이 더 높기 때문에 diffusion이 일어남)
# 양쪽의 chemical potential이 같아질 때까지 C의 diffusion이 일어나 결국은 양쪽 시편의 carbon 농도 차가 역전됨!
# Si는 substitutional diffusion을 하기 때문에 interstitial diffusion을 하는 C와는 달리 확산이 매우 느리게 진행된다!

## Slide 18: Ⅱ. 자유 주제 Growth of precipitation

## Slide 19: Nucleation and growth
Critical driving force & size
a
b
for spherical nuclei:
Critical radius
Critical driving force
stable size

## Slide 20: Growth of precipitation
Nuclei larger than V*(r*) will grow through interface migration
Shape of ppt depends on the migration rate of interface such as coherent, semi-coherent, and in-coherent
in-coh
coh/semi

## Slide 21: Growth of precipitation
Growth of planar incoherent interface
Diffusion controlled interface growth
Growth velocity (v) depends on (dC/dx) at interface
a
x
L
DCo
v
CB
x
b
Simplified approach :
Growth velocity :
Integration :

## Slide 22: Growth of precipitation
Overlapping diffusion field
High T -> small Dxo -> low v
Low T -> slow diffusion (low D) -> low v
∴ Maximum v at intermediate temp.
b
b
b
b
a
a
Composition & temp. dependence

## Slide 23: Problem setting
Postechium (Ps) - Kaistium (Ks) 2원계 상태도 (by Mid-term project)
Liquid
FCC(α)
FCC(α) + BCC(β)
FCC(α)+ L
BCC(β)+ L
T = 700.8K
BCC(β)
Xe = 0.079, Xβ = 0.907
Temperature after cooling = 700.8K
Diffusion coefficient
= exp[-147723(J)/RT]
(
Xe = 0.079
Xβ = 0.907
ΔT
ΔX0

## Slide 24: Result and analysis
X0 = 0.258 ( T0 = 1005K) 일 때, t = 100s 에서의 ppt growth
Xe = 0.079, Xβ = 0.907
Temperature after cooling = 700.8K
Diffusion coefficient
= exp[-147723(J)/RT]
(
Length of ppt = 4.547 nm
a
x
L
DCo
v
CB
x
b
b
a

## Slide 25: Result and analysis
시간에 따른 ppt growth
Xe = 0.079, Xβ = 0.907
Temperature after cooling = 700.8K
Diffusion coefficient
= exp[-147723(J)/RT]
(
X0 = 0.258 ( T0 = 1005K)
Length of ppt :
2.033nm(at 20s),
4.547nm(at 100s),
10.168nm(at 500s)
Length of ppt ∝ t

## Slide 26: Result and analysis
Maximum growth rate of ppt
Xβ = 0.907, X0 = 0.408 (T0 = 1500K)
Time = 100s
Diffusion coefficient
= exp[-147723(J)/RT]
(

## Slide 27: Result and analysis
Maximum growth rate of ppt
Xβ = 0.907, X0 = 0.408 (T0 = 1500K)
Time = 100s
Diffusion coefficient
= exp[-147723(J)/RT]
(
Maximum v at intermediate temp.

## Slide 28: conclusion
# FDM을 이용하여 incoherent interface 에서의 planar ppt growth를 성공적으로 simulatio할 수 있었다!
# 자유주제를 스스로 설정하고, 이를 해결함으로써 어떤 재료 열역학적 문제에 대해서도 수치해석적을 통해 분석할 수 있다는 자신감을 얻게 되었다!
# 단순히 이론적으로 주입식으로 받아들이고 이해했던 재료과학을 수치해석을 통해 직접 수학적으로 풀고 simulation해봄으로써 훨씬 이해도가 높아진 것 같다!

## Slide 29: 한 학기 동안 감사했습니다.