## Slide 1: Final Term project
20120778
Subin Lee

## Slide 2: Assignment

## Slide 3: Background
Multicomponent system에서의 diffusion coefficient는 (n-1) 차원의 행렬로 표현
각 원소의 Chemical potential

## Slide 4: Background
Initial value
Conversion wt% -> u fraction
Calculate diffusivity Si, C concentration
Algorithm
FDM(explicit method):

## Slide 5: Results
Carbon diffusion - Comparison with experimental results

## Slide 6: Results
Carbon diffusion - Time dependency

## Slide 7: Results
Si diffusion - Time dependency

## Slide 8: Results
Carbon diffusion - Temperature dependency

## Slide 9: Diffusion of Vacancies

## Slide 10: Introduction
Application of structural materials to MEMS/NEMS
→ Mechanical properties and deformation behaviors of nanomaterials
nanoindentation
Micropillar compression

## Slide 11: FIB induced damage
- 3 -
High energy (30keV) Ga+ ion beam induced damage
Various defect structures beneath the surface
Act as dislocation sources
Non-uniform contrast
Top-down approach
(FIB prepared Al pillar)
200 nm
TEM dark field images
Vacancy
Interstitial atom
Implanted atom
100 nm
Bottom up approach
(PVD grown Au NW)

## Slide 12: Annealing of FIB-induced damage
Thermal annealing by In-situ TEM heating
Annealing 20 min. @ 1/2Tm
Defect free single crystal pillar for characterization of mechanical properties & deformation behavior
10x played

## Slide 13: Shrinkage of dislocation loops
Dislocation line tension induces vacancy supersaturation
Vacancy diffusion
Shrinkage or expansion of the loops
D: diffusivity
G: shear modulus
b: Burgers vector
100 nm
(f)
t0
t0 + 753s
D1
D2
D3
D4
(a)
(b)
(c)
(d)
(e)
t0
420 K
t0 + 160 s
420 K
t0 + 280 s 420 K
t0 + 455 s 430 K
t0 + 753 s
440 K
Solve the differential equation
Distributed 100 dislocation loops with random radius
Annealing @ ½ Tm
Trace the change in radius of each loops

## Slide 14: Results
Small dislocation loops shrink whereas large loops expand
Average radius increases while dislocation density decreases
Similar to Ostwald ripening process for precipitates Vacancy diffusion process