## Slide 1: Problem 1. CSL boundary
Coincidence Site Lattice boundary
  Special high-angle boundary
  Partially coinciding points set
  Low misfit strain energy because of good atomic fitting
  Low grain boundary energy albeit high-angle boundary
20152027 조민국
Σ# : The reciprocal density of coincident lattice site

## Slide 2: Problem 2. General multicomponent form of solute composition in surface

## Slide 3: Problem 3. Abnormal grain growth
Grain growths affect by GB energy and GB mobility
AGG occurs at low grain boundary energy and high grain boundary mobility
Anisotropic grain boundary energy causes solid state wetting
  Ex) for grain A :
Triple junction wetting is a mechanism of AGG
Precipitates inhibits NGG by pinning effect at grain boundary -> Increasing high energy grain boundaries promote AGG possibility
Sub-boundaries increase triple junction wetting possibility by containing low energy grain boundaries -> Increasing AGG possibility
20152027 조민국